PCF fabricated at CGCRI, Kolkata

PCF – 19B

Fiber diameter = 123.45 (m

Air hole diameter = 5.06 (m

Pitch = 5.29 (m

Core diameter = 4.37 (m

Air filling fraction = 0.96