## Slide 1: Anisotropic Wet Etching of Silicon in a KOH Solution
COMSOL

## Slide 2: Model Setup
The anisotropic wet etching of silicon is simulated based on the different etching rates of silicon's crystal planes in the KOH solution.
The etching of the {100, 110, 111} crystal plane family is considered.
The anisotropic etching rate interpolation function is based on scientific literature [1].
The operating conditions are: 30% KOH solution at a temperature of 70°C, with the anisotropic etching rate values obtained from literature [2].
The shape of the etched groove on the 45° oblique section.
[1]Hubbard, Ted J. (1994) MEMS design : the geometry of silicon micromachining. Dissertation (Ph.D.), California Institute of Technology. doi:10.7907/TK4C-M144.
[2]Wagner, Andrew. (2005) KOH Si Wet Etch Review.

## Slide 3: Geometry
There is a small initial groove on the surface of the silicon wafer.
When the groove surface comes into contact with the KOH solution, the groove grows due to the chemical etching reaction.
groove surface

## Slide 4: Interpolation Function Based on the Normal Angle of Etching Surface and the Etching Rate of the {100,110,111} Crystal Plane

## Slide 5: Deformed Geometry
The Deformed Geometry feature is used.
Domain settings:
  Deforming domain
  Fixed domain
Boundary conditions:
  Groove surface: Prescribed Normal Mesh Velocity = -v_surface
  Surface of the deforming domain: Prescribed Normal Mesh Displacement = 0
Deforming Domain
Fixed Domain
Prescribed Normal Mesh Velocity: -v_surface
Prescribed Normal Mesh Displacement: 0

## Slide 6: Results
The etching depth increases gradually.
Etching is slower in the {111} crystal plane direction.
With the development of etching, V-shaped grooves are formed in the oblique plane.
The angle between the inclined edge of the V-shaped groove and the upper line is about 55 °, which is close to the theoretical angle of 54.736 ° between the (111) crystal plane and the (100) crystal plane.
45° oblique section
The shape of the etched groove change on the 45° oblique section.

## Slide 7: Results
Pyramid-shaped grooves are gradually formed over time.
Etched groove shape with time in 3D.

## Slide 8: Conclusions
The simulation of anisotropic wet etching of silicon in KOH can be achieved with the help of the Deformation Geometry feature in COMSOL® and a custom variable function.
Possible extension: The etching rate of the (311) crystal plane can be described using a detailed interpolation function in order to improve the model accuracy.